## Slide 1: Nanoscale thermal transport
Lecture 2
Riley Hanus
http://rileyhanus.com/science.html

## Slide 2
Define (and understand) the phonon band structures
Learn how to read a phonon band structure
Introduction to the phonon gas model
Derive the phonon density of states two ways

## Slide 3
Phonon band structures
Most solid-state physics classes will derive an analytical dispersion for a 1D chain.
If you haven’t seen this, read Kittel, Intro. to Solid State physics Chapter 4.
Much of the intuition gained from the 1D case extends to 3D
The math for a 3D crystal, which is used to calculate real dispersion relations is given in:
Wallace, Thermodynamics of Crystals, Chapter 3.10.
Hanus, Thesis, Section 2.2.1 and Appendix B.
Here we will outline the procedure for computing phonon properties:
frequencies
eigenvectors
(mode shape)

## Slide 4
Phonon band structures
Simply solve the equations of motion (Newton’s law)
: atom label
: direction
We know and ,
solve for .
Databases for interatomic force constants (IFCs) :
Phonopy: http://phonondb.mtl.kyoto-u.ac.jp/
almaBTE: http://www.almabte.eu/index.php/database/
Set up

## Slide 5
Expressing a function as a Fourier Series:
Required math
Type equation here.
and work
as do
and
Diagonalize
Matrix diagonalization:
Find ‘s and ‘s that obey this equation
(There are 3 combinations in this case since is 3 x 3)
( for phonons)

## Slide 6
Phonon band structures
1. Express as a Fourier Series (the Fourier coefficients “” are a bit more complicated here)
2. Solve equation of motion ()
2a. In solving we find its convenient to define the Dynamical Matrix
2b. Phonon ’eigenstates’ are the solutions you get when you diagonalize the Dynamical Matrix
Lattice Dynamics

## Slide 7
scalar
length vector
matrix
length vector
distinct and solutions
= # of atoms in unit cell

## Slide 8
Lattice dynamics quiz
Define interatomic force constants (IFCs).
How many IFCs are there?
Define the Dynamical Matrix.
What is its dimensions?
Define an eigenstate.
How many eigenstates are there at a given k-point?
Define an eigenvector.
What is its dimensions?
Define an eigenvalue
What is its ‘dimensions’?
N: number of atoms in the unit cell
3N x 3N
The frequency squared of the eigenstate
A vector denoting the atomic displacements in each cartesian direction of each atom in the unit cell (mode shape)
An eigenvalue/eigenvector set which diagonalizes the dynamical matrix
A matrix governing the dynamic (vibrational) properties of crystals
Ideally, you would have an infinite number.
The spring constants between all atoms in the crystal
3N
It’s a vector of length 3N (3N x 1)
It’s a scalar (so 1 x 1?)
key: 1g, 2f, 3e, 4a, 5d, 6g, 7c, 8i, 9b, 10j

## Slide 9
Phonon band structures
In practice
Find solutions (diagonalize the Dynamical Matrix)
Along special directions to plot
pretty band structures:
On a mesh to sample the entire Brillouin Zone, when we want transport properties of density of states:
Computational suites that do this:
phonopy: https://atztogo.github.io/phonopy/
almaBTE: http://www.almabte.eu/
shengBTE: http://www.shengbte.org/

## Slide 10
Reading a phonon band structure
acoustic modes ( at )
optical modes ( at )
is the number of atoms in the unit cell
Ultrasound, speed of sound,
Elastic tensor and moduli,
Bulk modulus, Young’s modulus,
etc.

## Slide 11
Reading a phonon band structure
Effect of atomic mass and the
phonon band gap.
Cubic GaN: N mass = 14 amu
Cubic GaAs: As mass = 75 amu
25 meV
25 meV
Units for vertical (energy) axis:
some use ‘angular’ frequency (they won’t show the rad though)
some use ‘ordinal’ frequency
some use frequency in
some use energy

## Slide 12
Ga: Brown
N: Blue
magnitude of atomic displacement dramatically exaggerated
https://henriquemiranda.github.io/phononwebsite/phonon.html

## Slide 13
magnitude of atomic displacement dramatically exaggerated

## Slide 14
magnitude of atomic displacement dramatically exaggerated

## Slide 15
Reading a phonon band structure
Group velocity and phase velocity
Phonon-gas model for heat flux:

## Slide 16
Wave packets
Group and phase velocity
https://www.youtube.com/watch?v=tlM9vq-bepA
https://demonstrations.wolfram.com/WavepacketForAFreeParticle/

## Slide 17
The phonon gas model
Lines are all:
DFT obtained interatomic force constants ( and )
Phonon properties from lattice dynamics
Thermal conductivity from the phonon gas model
First principles simulation, no adjustable parameters… but there are choices
McGaughey, A. J. H., Jain, A. & Kim, H. Phonon properties and thermal conductivity from first principles, lattice dynamics, and the Boltzmann transport equation. J. Appl. Phys. 125, 011101 (2019).
=
Notes: … except:
  what exchange correlation functional you decide to use
  what DFT parameters you use for and
    k-mesh density (hopefully converged)
    cutoff energy (hopefully converged)
  How you found all of the possible 3 phonon scattering processes (Gaussian smearing, search algorithm)
  How you perform your Brillouin zone integration
    uniform k-mesh? cylindrical k-mesh?
  Whether or not you included crystal boundary scattering, i.e. a maximum allowed mean free path
… except:
  what exchange correlation functional you decide to use
  what DFT parameters you use for Φ_𝑖𝑗^𝛼𝛽 and Φ_𝑖𝑗𝑘^𝛼𝛽𝛾
    k-mesh density (hopefully converged)
    cutoff energy (hopefully converged)
  How you found all of the possible 3 phonon scattering processes (Gaussian smearing, search algorithm)
  How you perform your Brillouin zone integration
    uniform k-mesh? cylindrical k-mesh?
  Whether or not you included crystal boundary scattering, i.e. a maximum allowed mean free path

## Slide 18
The phonon gas model
Mode specific treatment:
(computational approach)
Spectral treatment:
(Callaway modeling)
Where we define:
The spectral model can be thought as containing the mode specific properties “under the hood”.
Often, in real (defective) materials, we don’t have access to full mode specific properties, and therefore use the spectral treatement.

## Slide 19
The phonon gas model

## Slide 20
Density of states
Cubic GaN
How many states are at given energy?
where group velocity goes to zero at the BZ edge = “Van Hove singularity” = peak in density of states
,
When branches are linear

## Slide 21
Density of states
Probably the most common derivation.
: number of states
: crystal volume
: magnitude of the k-vector
: volume of k-space
: number of states per volume
: a definition of the phonon density of states
assert a Debye model for phonon dispersion relation (band structure):
We will just examine one branch.
Notice:
This derivation does not
predict Van Hove singularities

## Slide 22
Density of states
Another derivation which is a more informative and will introduce us to some math which is important in scattering theory
Note the units:
if (and therefore ) has units of
then has units of
Integrating over delta functions:
Converting sums to integrals:
The sum introduces no units.
The integral comes with , which has a value of after integrating over the FBZ.
Instructive exercise:
Pretend and compute both.
Hint:
Required math:
: number of k-vectors considered in the sum
: is the volume of the unit cell

## Slide 23
Density of states
A second definition of the density of states:
(1) pick a frequency/energy
(2) search through the whole FBZ and count all modes at that energy
large DOS
small DOS

## Slide 24
Density of states
For comparison we will only look at one branch, so only .
Therefore, we don’t need the sum over .
Convert sum to an integral
Cancel , and switch to spherical coordinates.
on board

## Slide 25
Density of states
Now we make the isotropic assumption, by saying that no longer depends on the direction is pointing, but only on its magnitude .
After this, we can take the integrals over and :
Need to convert the integral such that its over so we can take advantage of that -function. We use our definitions of group and phase velocity to do this.
Finally, we take the integral.
on board

## Slide 26
Density of states
For a linear dispersion
keep in mind and
can change with
When ,
and that is our
Van Hove singularity
(same as first derivation)
Currently we are only looking at
only one branch. Sometimes we approximate all three acoustic branches as one branch with average group and phase velocities.
on board