## Slide 1: Nanoscale thermal transport
Lecture 5
Riley Hanus
http://rileyhanus.com/science.html

## Slide 2
Wavelength, coherence length, mean free path, and relaxation time
Example Callaway model
Explore how different scattering mechanisms influence thermal conductivity versus temperature
  Point defects
  Interfaces
Explore low and high temperature limits
  Lattice softening
Mean free path accumulation

## Slide 3
Review wave packet basics

## Slide 4
Review wave-packet basics
Relaxation time, (scalar): The time between scattering events of a phonon wave-packet.

## Slide 5
Review wave-packet basics
Group velocity, (vector): The speed and direction the wave-packet travels.

## Slide 6
Review wave-packet basics
Mean free path, (vector): The distance a phonon wave-packet travels before scattering.
determines how closely defects must be space for them to significantly reduce thermal conductivity. For example, defects that are spaced significantly farther apart than the phonon wave-packets phonon-phonon scattering mean free path, will not significantly reduce the heat carried by the wave-packet.

## Slide 7
Review wave-packet basics
Wavelength, (vector): The wavelength of the wave-packet.
, influences how strongly the phonon wave-packet will interact with a defect of a given physical size. This is intuitive when one remembers the scattering rate involves the real space Fourier transform of scattering potential (Lecture 4).

## Slide 8
Review wave-packet basics
Coherence length (vector): The distance over which the atomic vibrations are correlated to one another.
Ideal plane waves have an infinite coherence length. These do not exist in nature. In reality, there is a distance beyond which the vibration of atoms are uncorrelated.

## Slide 9
Callaway Modeling
We’ve derived each part of this model in previous lectures.
The spectral version is listed here for reference.
A similar procedure can be performed on a mode specific basis.
Dispersion relation:
1) Debye
2) Born von Karman
only acoustic modes
: volume per primitive unit cell
all modes
volume per atom
Anderson, O. L. J. Phys. Chem. Solids 24, 909–917 (1963).

## Slide 10
Example Callaway model
phonon-phonon scattering
point defect scattering
kg/mol
kg/mol
boundary scattering
Materials values required to reproduce this model
(roughly based on Si)
Tan, G. et al. ACS Energy Lett. 3, 705–712 (2018).
Hanus, R., Garg, A. & Snyder, G. J. Commun. Phys. 1, 78 (2018).

## Slide 11
Low-T gives information about microstructural scattering
High-T, behavior stems from phonon-phonon scattering
Example Callaway model
T 3
T -1
Notes: Check units!!

## Slide 12
Example Callaway model
Increased point defect scattering

## Slide 13
Example Callaway model
Increased microstructural scattering

## Slide 14
Example Callaway model
Comparing the previous two models
increased point defect scattering vs. increased microstructural scattering

## Slide 15
Low-temperature limit
exercise
assert Debye dispersion:
Debye-Callaway model:
Callaway (spectral) model:

## Slide 16: Low-T of polycrystalline materials
Wang, Z., et al. Nano Lett. 11, 2206–2213 (2011).
Berman, R. Proc. Phys. Soc. Sect. A 65, 1029–1040 (1952).
Watari, K. et al. J. Mater. Res. 17, 2940–2944 (2002).
cst @ low-T
Case 1:
Low-temperature limit
Hanus, R., Garg, A. & Snyder, G. J. Phonon diffraction and dimensionality crossover in phonon-interface scattering. Commun. Phys. 1, 78 (2018).
on board

## Slide 17: Low-T of polycrystalline materials
Wang, Z., et al. Nano Lett. 11, 2206–2213 (2011).
Berman, R. Proc. Phys. Soc. Sect. A 65, 1029–1040 (1952).
Watari, K. et al. J. Mater. Res. 17, 2940–2944 (2002).
Case 2:
cst @ low-T
Low-temperature limit
Hanus, R., Garg, A. & Snyder, G. J. Phonon diffraction and dimensionality crossover in phonon-interface scattering. Commun. Phys. 1, 78 (2018).
on board

## Slide 18
High-temperature limit
Hanus, R. et al. Lattice Softening Significantly Reduces Thermal Conductivity and
Leads to High Thermoelectric Efficiency. Adv. Mater. 1900108, 1900108 (2019).
Assert the following form of phonon-phonon scattering, and Debye dispersion
Make high temperature approximation () for
exercise
Refs: Slack, G. A. & Galginaitis, S. Phys. Rev. 133, (1964).
Toberer, E. S., et al. J. Mater. Chem. 21, 15843 (2011).

## Slide 19
Phonon scattering vs. Elastic (lattice) softening

## Slide 20
When is softening expected to be important?
Anharmonic materials
High temperatures
800 K, phonon-phonon scattering dominates

## Slide 21
Accumulation plots
If I know , then I can rewrite the integral over to one over .
Note, usually decreases with increasing .
So we label and
Yang, F. & Dames, C. Mean free path spectra as a tool to understand thermal conductivity in bulk and nanostructures. Phys. Rev. B - Condens. Matter Mater. Phys. 87, 1–12 (2013).
Flip the limits, which spits out a negative sign, and package up the integrand into
Now define the “Normalized accumulation function”
plot from to
on board

## Slide 22
Intrinsic phonon mean free path
Liu, Z., Mao, J., Liu, T.-H., Chen, G. & Ren, Z. MRS Bull. 43, 181–186 (2018).
PbTe
~ 5 nm
Si
~ 1000 nm
Accumulation plots
75% of the heat is carried by phonons with a mean free path less than 1000 nm in Si, and less than 5 nm in PbTe
Example